PART 1 - GENERAL

1.1	RELATED SECTIONS:

  - SCOPE OF SECTION:

This section contains the requirements relating to corner guards.

  - CORNER GUARDS:

- Snap-on covers of .080 thickness extruded from chemical and stain resistant polyvinyl chloride with the addition of impact modifiers.

- No plasticizers shall be added (plasticizers may aid in bacterial growth).

- Surface shall have embossed texture.

- End caps and outside corners shall be made of injection molded thermoplastics of color matching that of wall guard.

- Continuous aluminum retainer shall be fabricated from 6063-T5 aluminum, with a mill finish.

END OF SECTION